Co-axial Jelly

| Sr. # | Characteristic | Specifications |
| --- | --- | --- |
| 1. | Colour | Light Yellow |
| 2. | Handling | Easily Removable |
| 3. | Stability @ 65oC / 5 days | Passes |
| 4. | Toxicity | Certified by Indian Institute of Toxicity |
| 5. | Drop Point oC | 100 - 115 |
| 6. | Flash Point (COC) oC | 220 min |
| 7. | Neturalisation No. mg KOH/g | 0.03 |
| 8. | Cone Penetration @ 25oC (dmm) | 60 - 70 |
| 9. | Volume Resistance @ 100oC/500 VDC, Ohm - cm | 4.40 x 1013 |
| 10. | Permitivity @ 20oC, 1 Mhz | 2.08 |
| 11. | Power Factor @ 20oC, 1 Mhz | 0.0005 |
| 12. | OIT @ 190oC, Cu Pan Minutes | >/= 30 |

For further information please send us an Email on sales@paraffinoil.com