Natural Beeswax Specifications

| Test/Method | Method | Typical Specifications |
| --- | --- | --- |
| Drop Melting Point | ASTM D-127 | 70 - 80° C |
| Needle Penetration At 25° C |  | 25 – 45 |
| Colour (Max) | ASTM D-1500 | 0.0 – 0.5 (Max) |
| Oil Content | ASTM D -721 | Less than 2.0 |
| Flash Point (Coc) | ASTM D – 92 | 260° C |
| Viscosity @ 98.9° C | P: 25 | 15 – 20 Cst |
| UV visible Absorption | ASTM D-2008 | Passes Test |
| Odour |  | Odourless |
| Acidity & Alkalinity | P: 2 | Passes Test. |
| Residue on Ignition |  | Passes Test |
| Organic Acids |  | Passes Test |
| Fixed Oils, Fats & Rosins |  | Passes Test |

For further information please send us an Email on sales@paraffinoil.com

The information provided on this page is, to the best of our knowledge accurate, however, it is subject to change without prior notice.  We assume no liability for the completeness of it or errors in it.  Current and final specifications and datasheets can be obtained by contacting us on sales@paraffinoils.com